# Pos.	Quantity	Unit	Article/work			Unit price EUR	 	Total EUR

transfer:		_______,____

2.				Plastifloor-coating

2.01			m²	Prime prepared surface until all

pores are sealed.

Material:		Plastifloor 112

Material consump:	0.5 kg/m² per layer until

all pores are sealed

Broadcast with quartz sand 0.2-0.7 mm.

_______,____		_______,____

OPTION

2.02			kg/h	Levelling works

Deep or large holes and cavities,

eruptions or extreme flaws in the

substrate are eliminated in advance

on site or on customer’s directive

by our staff on direct labour, with

wage and material cost statement.

1 technician work hour:

1 kg resin-based mortar 510/1:

An even floor coating, corresponding

to  DIN 18202, can only be achieved if

a correspondingly even substrate

exists or is established on customer’s

directive.		_______,____		_______,____

OPTION

2.03			kg/h	If there is no sufficient slope on site

(~ 2 %), this can be installed with reactive

resin-based mortar on customer’s directive

by our staff on direct labour, with

wage and material cost statement.

If the coating is installed without

sufficient slope, puddles on the floor

cannot be excluded.

____________

Continued on page 3						transfer:		_______,_____

# Pos.	Quantity	Unit	Article/work			Unit price EUR	 	Total EUR

transfer:		_______,____

1 kg resin-based mortar 510/1:

1 h processing time:		_______,____		_______,____

OPTION

2.04			m	Force-fitly cast elaborated construction

joints and cracks.

Joint dimension:

Material: 	Plastifloor 510

Consumption:	   kg/m		_______,____		_______,____

2.04a			m	Form elaborated expansion joints

in the structure permanently elastic.

or install a suitable metal joint profile.

Joint dimension:

Material.	Plastifloor 430

Consumption:	   kg/m		________,____	________,____

2.05			m²	Apply an impermeable, crack-bridging

Compensating membrane onto the

primed surface by using a trowel and

broadcast with fire-dried quartz sand.

layer thickness:	2 – 3 mm

Material:		Plastifloor 332/Z

Material consump:	2.5 kg/m²												Plastifloor 332/Z

_______,_____	_______,____

2.06			m²	Apply the Plastifloor broadcast coating

with a toothed squeegee and draw off,

de-aerate with a spike roller if required								layer thickness:	~ 4 mm

Material consump:	~ 3 kg Plastifloor 410,

filler:			~ 2.1 kg quartz sand 0.06 – 0.2 mm

Broadcast the coating when still wet with:

~ 5 kg colour sand

0.7 – 1.2 mm

Slip resistance R 12 – R 13

_____________

Continued on page 4					transfer:			_______,_____

# Pos.	Quantity	Unit	Article/work			Unit price EUR	 	Total EUR

transfer:		_______,____

Colour sand S 1 – S 12 or 417

Due to the manufacturer, colour and

mixture deviations are possible. They

do not lead to warranty claims.

_______,____		_______,____

Manufacturer:

Plasti-Chemie International GmbH

Zum Plom 35

08541 Neuensalz

-------------------------

phone: 03741/5583-0

fax: 03741/558327

    - m²       Seal the coated surface.

Sealing must be effected until all

pores are sealed.

Material:		Plastifloor 526

Material consump:	0.5 l/m²

_______,____		_______,____

2.08			m	Form a surface-finished cove, with installation

of an edged stainless steel profile, on all

opening walls. Seal the profile edge on

the top with PU-sealant.

Material: Plastifloor 510/H, colour quartz sand

Height:	  ~ 5 cm as per EU-Norm

Colour: like floor surface	_______,____		_______,____

3.				Site equipment

3.01			all in	Setting up the site, provide tools

Machines during the whole con-

struction period.

- Executing and recording CM-measuring

- Executing and recording 1 bond strength

measurement

- Dispose of empty bundles environmentally

friendly

- Approach and departure from site 1 x

- Expense allowance for our staff

_______,____		_______,____

_____________

Continued on page 5					transfer:			_______,_____

# Pos.	Quantity	Unit	Article/work			Unit price EUR	 	Total EUR

transfer:		_______,____

TITLE SUMMARY

Floor preparation

Plastifloor-coating

Site equipment					____________

Net amount						_______,____

VAT		_____ %		_______,____

-------------------

Total amount 					_______,_____

===================================================